Te**chnical Product Data sheet**

Product Name: Plasbond

Product description: Flexible water borne smooth masonry coating based on a modified VA polymer. Provides long term decoration and protection to most masonry

surfaces. (Note: Fletton Commons should not be painted). Plasbond

contains a fungicide to inhibit mould growth on the surface and provides excellent long term flexibility and weather resistance

Uses: Decoration and protection of a wide range of masonry surfaces

Pack sizes availability:5, 10 litres

Colour range: White and a selection of BS4800 colour. Special colours on request

subject to minimum batch sizes

Specific gravity: Approx 1.33

Flash point: Non flammable

Recommended Spreading rate: 3m²/litre applied over two coats

Solids content: Approx 50% w/w Approx 38% v/v

Drying time: Approx 2-4 hours 20°C 65%RH

Over-coating time: Approx 6-8 hours 20°C 65%RH

Minimum application temperature: Air and surface temperature should be 5

°C and rising. Do not apply during damp or frosty weather or when rain is imminent

Recommended dry film thickness: Approximately 130microns

Method of application: Brush, roller or airless spray

Preparation: Surfaces must be clean, sound and dry and prepared in accordance with BS6150 Painting of buildings –code of practice.

Surfaces which remain chalky or dusty after preparation should be coated

with stabilising solution (S/B or W/B). Treat organic growth with fungicidal solution.

Bare metal surfaces must be adequately primed.

Storage life: Min 12 months in original sealed containers. Protect from frost and direct

heat

Thinning/cleaning: Thin where necessary with clean water. Do not exceed 1 part water to 10 parts of Plasbond.Wash equipment immediately after use with water and detergent

Safety precautions: Refer to the safety data sheet before use

Volatile organic content (voc) Limit for this product: Cat A/c 40g/l (2010).

This product contains maximum 5g/l VOC

Disposal: As supplied or containing liquid product–non hazardous waste code

08 01 12 waste paint and varnish other than those mentioned in 08 01 11

Used containers drained/rigorously scraped out and containing only dry

residues: categorised as non-hazardous with waste code 15 01 02 (plastic package)

and 15 01 04 (metal package)